## Slide 1
Declaration of Performance (according to Construction Product Regulation EU No 305/2011) No. Plate S355J2W Plate S355J2W / 1.8965 according EN 10025-5 To be used in Metal Structures and Composite Metal and Concrete Structures Liberty Steel Dalzell Limited Park Street, Motherwell, ML1 1PU United Kingdom Tel: +44 (0)1698 266100 Website: www.libertyhg.com/Dalzell CE Marking Notified Body Lloyds Register Verification B.V K.P van der Mandelelaan 41A Tel: +31 (0)10 4145088 Lloyd’s Email: Rotterdam@lr.org System of assessment and verification of constancy of performance of the product System 2+ Notified factory production control certification body No. 2814 performed the initial inspection of the manufacturing plant and of factory production control and the continuous surveillance, assessment, and evaluation of factory production control and issued the certificate of conformity of the factory production control Signed for and behalf of Liberty Steel Dalzell Ltd; Name: Kenny McLeary Title: Technical Manager Sign: Date
2814
Liberty Steel Dalzell Limited Park Street, Motherwell, ML1 1PU United Kingdom 16 Plate S355J2W
EN 10025-1 – 2004 Plate S355J2W / 1.8965 To be used in Metal Structures and Composite Metal and Concrete Structures Tolerances on dimensions: Plate EN10029 Elongation: Tensile Strength: Yield Strength: EN10025-5 Impact Strength: Weldability: Durability: Dangerous Substances: No Performance Determined
Essential Characteristic | Performance |  |  |  | Harmonised Technical Specification
Tolerances on dimensions & shape | Thickness |  | EN 10029 |  | EN1005-1 2004
 | Flatness |  | EN 10029 |  | 
Yield strength (transverse) | Nominal Thickness (mm) |  | Values Min (Mpa) |  | 
 | > | <= |  |  | 
 | - | 16 | 355 |  | 
 | 16 | 40 | 345 |  | 
 | 40 | 63 | 335 |  | 
 | 63 | 80 | 325 |  | 
 | 80 | 100 | 315 |  | 
 | 100 | 150 | 295 |  | 
Tensile strength (transverse) | Nominal Thickness (mm) |  | Values (Mpa) |  | 
 | > | <= | Min | Max | 
 | 5 | 100 | 470 | 630 | 
 | 100 | 150 | 450 | 600 | 
Elongation (transverse) | Nominal Thickness (mm) |  | Values Min (%, 5.65√so) |  | 
 | > | <= |  |  | 
 | 0 | 40 | 20 |  | 
 | 40 | 63 | 19 |  | 
 | 63 | 150 | 18 |  | 
Impact strength (longitudinal) | L |  | 27J at -20°C |  | 
Weldability CEV | Nominal Thickness (mm) |  | Values Max (%) |  | 
 | > | <= |  |  | 
 | - | 63 | 0.52 |  | 
 | 63 | 100 |  |  | 
 | 100 | 150 |  |  | 
Durability | Nominal Thickness (mm) |  | Values Max (%) |  | 
 | 0 | 150 | C: 0.16 |  | 
 |  |  | Si: 0.50 |  | 
 |  |  | Mn: 0.5 – 1.50 |  | 
 |  |  | P: 0.030 |  | 
 |  |  | S: 0.030 |  | 
 |  |  | Nb: 0.015 – 0.060 |  | 
 |  |  | V: 0.02 – 0.12 |  | 
 |  |  | Ti: 0.02 – 0.10 |  | 
 |  |  | Cr: 0.40 – 0.80 |  | 
 |  |  | Ni: 0.65 |  | 
 |  |  | Mo: 0.30 |  | 
 |  |  | Cu: 0.25 - 0.55 |  | 
 |  |  | N: 0.009 |  |